## Slide 1
Luminescence behaviors of Sm3+ doped high density tungsten gadolinium borate scintillating glass
Jakrapong Kaewkhao
Center of Excellence in Glass Technology and Materials Science (CEGM)
Nakhon Pathom Rajabhat University, Nakhon Pathom, Thailand

## Slide 2
Topic
GlassLab@NPRU
Application of Radiation Detection Materials
Concept of Glass
Luminescence from Ln3+
Glass Preparation
Result and Discussion
XRD, Density, Molar Volume
Transmission Spectra
Excitation and Emission (Photo, X-rays and Protron induced luminescence)
Temperature dependence (down to 10 K)
Decay time (PL and X-rays excitation)

## Slide 5
High Energy / Nuclear Physics
Radiation Detecting Material Application
Radiation Monitoring
Homeland Security
Neutron Imaging
X-ray imaging
2

## Slide 6
Radiation
Scintillation crystal
Radiation detection (bulk) material
CsI:Tl
BGO
NaI:Tl
3

## Slide 8
Single crystal and Glass
4

## Slide 9: Luminescence properties of Ln3+
Ln3+
Photon
Excitation factor
Photon
Electric current
Chemical reaction
Neutron
etc (not heat directly)
Intense emission
Stable in difference host
4f-4f transition
5s & 5p
4f
Ln3+ | Emission (nm) | τ
Sm3+ | ~600 | ms
Dy3+ | ~483 and ~575 | ms
Eu3+ | ~613 | ms
Nd3+ | ~1050 , λ/2 to Green | μs
Tb3+ | ~544 | ms
Ce3+ | ~350 | ns
5

## Slide 10
The necessary properties of X-ray / neutron detection material
Good transparent (Borate glass)
Good interaction with X-ray (W & Gd) and neutron (B & Gd)
Good energy transfer from host to luminescence center (Gd3+)
Strong emission (Sm3+)
High density (W)
Glass for X-ray/neutron detection
6

## Slide 11
Composition of Glass
Gd
W
B
42.5WO3 ˗ 27.5Gd2O3 ˗ (30-x)B2O3 ˗ xSm2O3 Glass
Carel W.E. van Eijk, Inorganic scintillators for thermal neutron detection, Radiation Measurements 38 (2004) 337 – 342.
Gang Ho Lee, Yongmin Chang, Tae-Jeong, 2 - Properties and possible application areas, Ultrasmall Lanthanide Oxide Nanoparticles for Biomedical Imaging and Therapy (2014) 15–28.
Y. Taki, K. Shinozaki, T. Honma, V. Dimitrov, T. Komatsu, Journal of Solid State Chemistry 220 (2014) 191–197.
N. Wantana, S. Kaewjaeng, S. Kothan, H.J. Kim, J. Kaewkhao, Journal of Luminescence 181 (2017) 382–386.
N. Wantana, E. Kaewnuam, Y. Ruangtaweep, D. Valiev, S. Stepanov, K. Yamanoi, H.J. Kim, J. Kaewkhao, Radiation Physics and Chemistry 164 (2019) 108350.
Borate
Borate compound is a suitable host glass with high transparency, high thermal stability, low melting point and good solubility of lanthanide ions.
10B can interact to thermal neutron with high capture cross-section
Tungsten
Tungsten are important due to increase density and decrease phonon in the glass.
Sm
7
Where x is 0.0, 0.1, 0.5, 1.0 and 2.0 mol%
Gd3+ as sensitizer
Good for capturing the neutron, X-ray and γ- ray
Transfer energy to Ln3+
Sm3+ as luminescence center
Strong orange emission
Decay time in ms

## Slide 12
Objective
- To prepare high density glass and study their luminescence behaviors for radiation detection materials application

## Slide 13
Weight
Melt
Anneal
Poured into preheat stainless steel mould
Put alumina crucible in Electric Furnace
500 ̊C
Glass Preparation
1200 ̊C
42.5WO3 ˗ 27.5Gd2O3 ˗ (30-x)B2O3 ˗ xSm2O3 Glass
Where x is 0.0, 0.1, 0.5, 1.0 and 2.0 mol%
8

## Slide 14
UV-3600 Shimadzu Spectrophotometer
Absorption spectra
Cary Eclipse Fluorescence Spectrophotometer
Photoluminescence (PL)
Temperature-dependent Luminescence
Analytical instrument
4-digit sensitive microbalance A&D HR-200
ρ; Archimedes principle
9
XRD
(XRD) (Shimadzu XRD-6100)
X-Rays Induced Optical Luminescence (Raidolumenescence; RL)
X-ray source was operated
at 50 kV and 30 mA
Pulse X-ray decay curve
Pulse x-ray 20 ns

## Slide 15: XRD, Density & Molar Volume
Fig. (a) XRD pattern of 2.0Sm:WGB glass and (b) density and molar volume of Sm:WGB glasses.
The XRD pattern confirms the weak of crystalline phase that indicates
the amorphous nature of the glass system.
(a)
10
(b)
Density
5.986 – 6.180 g/cm3
Molar volume
36.647 – 36.360 cm3/mol

## Slide 16: Transmission Spectra
Fig. (a) The transmission of the Sm:WGB glasses.
11
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.
Glass samples absorbed photon in VIS and NIR region

## Slide 17
11
Excitation Spectra

## Slide 18
11
Excitation Spectra (with/without WO3)
With WO3
42.5WO3 ˗ 27.5Gd2O3 ˗ (29-x)B2O3 ˗ 1Sm2O3 Glass
Without WO3
70Gd2O3 ˗ (29-x)B2O3 ˗ 1Sm2O3 Glass

## Slide 19: Photoluminescent spectra (with WO3, Vary Sm2O3 concentration)
Concentration quenching effect
Intensity of emission is highest at
1.00 mol% Sm2O3 doped glass
Glass show the strongest emission with 600 nm
Under 275 nm excitation
Under 311 nm excitation
Under 403 nm excitation
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.
12

## Slide 20: Photoluminescent spectra (with/without WO3)
Under 275 nm excitation
Under 311 nm excitation
Under 403 nm excitation
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.
12

## Slide 21: The emission intensity & Energy diagram
Fig. (a) The emission intensity of 600 nm under all three wavelengths excitation as a function of Sm2O3 concentration and
(b) Energy levels diagram of Gd3+ and Sm3+ ions in the WGB glasses for PL emission spectra.
(a) (b)
13
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.

## Slide 22
Decay curve
Fig. Decay curves of the Sm:WGB glasses for 600 nm emission under 275 nm excitation
14
Glass | τ (ms) | Q | R2
0.1Sm:WGB | 1.244 | - | -
0.5Sm:WGB | 0.957 | 0.350 | 0.992
1.0Sm:WGB | 0.695 | 0.718 | 0.994
2.0Sm:WGB | 0.414 | 1.370 | 0.987
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.
Table. Lifetime (τ) and energy transfer parameter (Q)
and R-squared (R2) of the Sm:WGB glasses
The energy transfer parameter (Q) that relates to the probability of energy transfer between Sm3+ ions.

## Slide 23: Temperature dependent luminescence
Fig. (a) the temperature dependent luminescence spectra and (b) Energy diagram of temperature dependent luminescence in the 1.0Sm:WGB glass
Journal of Luminescence 181 (2017) 382–386, Applied Physics B 98 (2010) 417–421.
15
The emission intensity at 10 K is higher than the intensity at 300 K around 3.76 times
(a) (b)

## Slide 24: CIE 1931 Chromaticity
Under laser excitation
(405 nm)
Under UV lamp excitation
16

## Slide 25: X-rays induced optical luminescence
Fig. (a) RL spectra of the Sm:WGB glasses (b) RL decay curve of the 1.0Sm:WGB glass.
17
Journal of Luminescence 181 (2017) 382–386
(a) (b)
The obtained fast (τ1) and slow (τ2) luminescence decay time of glass is
0.020, and 0.268 ms, respectively.

## Slide 26: Proton Luminescence
Glass show the strongest emission with 650 nm (4G5/2 →6H9/2)
Fig. protonluminescence spectrum of the 1.0Sm:WGB glass.
Emitted photons with 4 wavelengths via similar transitions in the RL spectra.
1.0Sm:WGB glass
18
Journal of Luminescence 181 (2017) 382–386,

## Slide 27: Conclusion
Scintillating Sm:WGB glass are very heavy, having densities up to 6.18 g/cm3.
For photoluminescence, energy transfer from Gd3+ to Sm3+ resulted to the strongest emission around 600 nm of Sm3+ (4G5/2 →6H7/2).
For the X-ray induced optical and proton luminescence, the emission spectra were nearly identical to those of the PL, but strongest intensity at 650 nm (4G5/2 →6H9/2) wavelength. (PL is strongest at 600 nm peak)
The optimum concentration of Sm2O3 for WO3-Gd2O3˗B2O3 glass is 1.0 mol% which performed the highest emission intensity in these two types of luminescence spectra.
The emission intensity of glass increased 3.7 times, with temperature down to 10 K)
The decay time under pulse X-ray excitation is 0.268 ms that is in the same order of photoluminescence decay time.
These glasses perform a potential for applications in the high energy / nuclear physics, radiation monitoring and homeland security.
19

## Slide 28: Acknowledgements
The Royal Golden Jubilee (RGJ) Ph.D. Program (Grant No. PHD/0100/2559)
Prof. HongJoo Him, Department of Physics, Kyungpook National University, Daegu, Republic of Korea
20

## Slide 29
Thank you for your attention