## Slide 1
Optimization and Enhancement of CNR in MRI using Core/Shell Contrast Agents
D. MacDonald [1], B. Blasiak [1] [2], B. Tomanek [1] [2] [3]
References:
[1] J. P. Hornak, “The basics of MRI,” CHAPTER-10. [Online]. Available: https://www.cis.rit.edu/htbooks/mri/chap-10/chap-10.htm. [Accessed: 08-Oct-2021].
[2] Huang, T., Huang, I., Chen, C., Scheffler, K., Chung, H. and Cheng, H., 2002. [online] Mriquestions.com. Available at: <http://mriquestions.com/uploads/3/4/5/7/34572113/are_truefisp_images_t2t1-weighted.pdf> [Accessed 8 October 2021].
Introduction:
Magnetic resonance imaging (MRI) provides the best soft contrast tissue among diagnostic imaging modalities such as CT, PET or X-ray. The contrast provided by MRI is based on the proton density and on interactions of protons with the surrounding molecules of tissues causing so called and relaxations. MRI techniques utilize these processes for contrast manipulation by producing or weighted MR images. While MRI contrast may be provided solely by tissues themselves due to differences in their relaxation times, contrast agents shortening and further improve detection of small pathologies such as early stages breast or brain cancers. Recently / core shell contrast agents have been developed with an expectation that the contrast to noise ratio () would be greater than when compared to no contrast agent, contrast agent. The advantages of some of these core shell contrast agents over core-only contrast agents include lower toxicity, greater dispersibility, greater biocompatibility, easier conjugation with other bioactive molecules, and increased thermal and chemical stability.
=|(1-|
=|(1-| [1]
Eq 1,2
Methods:
Optimization:
Assuming a known and relaxation for tumor and normal tissue, we calculated optimal (echo time) and (repetition time) for SE and IR TrueFISP to obtain the maximum .
Spin Echo (SE):
The optimization was obtained by allowing and to find the maximum . The signal from the tissues and tumors were calculated as follows for SE:
=|(1-2+|
[2]
Eq 3,4
IR TrueFISP:
Optimization for IR TrueFISP pulse sequence was done by ranging , and . Where is the inversion time. The Signal in completely balanced IR TrueFISP sequence can be seen below
Where , is the longitudinal relaxation for both the tumor and the tissue, is the transverse relaxation for both the tumor and the tissue.
Where and is the flip angle.
Conclusions:
The results show that the of a tumor for a / core shell contrast agent is greater than that of no contrast agent, contrast agent and a contrast agent for both the Spin Echo and IR TrueFISP pulse sequences. To demonstrate the potential of our core/shell contrast agent in vivo MRI we imaged mice with breast tumors before and after intravenous injection of 0.25 mL of non-targeted core shell contrast agent NaDyF4 (20 nm)/NaGdF4 (~ 0.5 nm). Then to further increase the , we subtracted a weighted image with weighted image. Pre injection results show that the best is from the weighted image, then the next best is from the w - image and lastly the w image. Post-injection results show that the best comes from the weighted image subtracted by the weighted image, and the for the weighted image is greater than the for the weighted image.
Eq 5
Results:
SE Optimization:
Table 1 and the graphs below show the maximum for a spin echo pulse sequence, using the optimal , . This is based off of equation 1, 2, and 5:
Table 1, Figure 1: Calculated maximum of a SE pulse sequence before injection of contrast and after injection of and contrast agent based on our data.
IR TrueFISP Optimization:
The table and the graphs below the optimal , to generate the highest for a FISP pulse sequence, and is based off of equation 3, 4, and 5:
Table 2, Figure 2: Calculated maximum , for the particular and values of a IR TrueFISP pulse sequence before injection of contrast and after injection of and contrast agent based on our data, flip angle alpha=0.261rad (15 deg).
Invivo Image Subtraction:
To demonstrate the potential of our core/shell nanoparticles in in vivo MRI, we did a w and a w image on animals with breast tumors before and after intravenous injection of 0.25 mL of non-targeted core shell contrast agent NaDyF4 (20 nm)/NaGdF4 (~ 0.5 nm). We then tried to increase the CNR by subtraction the w image with the w image. The images can be seen below:
Figure 3: Breast tumor (TNB), from left to right, image A is a w image pre injection, image B is a w pre-injection, image C is the subtraction of both images. The red indicates the tumor, blue indicates the tissue.
-
=
Figure 4: Breast tumor (TNB), from left to right, image D is a w image post injection (NaDyF4/NaGdF4), (injection of what), image E w post injection and image F is the subtraction of both images. The red indicates the tumor, blue indicates the tissue.
Table 3 below shows the signal acquired from both the tumor and the tissue as well as the for figures 3 and 4.
Table 3. Calculated maximum for the particular weighted, weighted and weighted - weighted images, for both pre-injection and post-injection of a 0.25 mL non targeted contrast agent, from figures 1 and 2.
CNR:
The CNR was calculated in the following way:
-
=
Images after Injection T1/T2 Contrast Agent:
A
B
C
D
E
F
The results from table 1 and figure 1 shows that the maximum is greatest from the / contrast agent, then from the agent, then from contrast agent and the west comes from when there is no contrast agent injected.
In vivo Image Subtraction
To demonstrate the potential of our core/shell nanoparticles in vivo MRI, we imaged animals with breast tumors after intravenous injection of 0.25 mL of non-targeted core shell contrast agent NaDyF4 (20 nm)/NaGdF4 (~ 0.5 nm), with a weighted pulse sequence (SE) and a weighted pulse sequence (IR TrueFISP). We then subtracted the w with the w image.
The results from table 2 and figure 2 shows that the maximum is greatest from the / contrast agent, then from the agent, then from west comes from when there is no contrast agent injected.
The results from table 3 shows the for a w, w, w- w image before and after contrast. Before the intravenous injection of 0.25 mL of non-targeted core shell contrast agent NaDyF4 (20 nm)/NaGdF4 (~ 0.5 nm), the highest was that from the w image, secondly was the from the subtracted images and lastly the from the w image. After the intravenous injection of 0.25 mL of non-targeted core shell contrast agent NaDyF4 (20 nm)/NaGdF4 (~ 0.5 nm), the results show that the highest CNR was that from the subtracted image, secondly was the CNR from w image and lastly the from the w image.
Before injection of contrast | After injection of contrast | After injection of contrast | After injection of / contrast
Before injection of contrast |  |  | 
Before injection of contrast | After injection of contrast | After injection of contrast | After injection of / contrast
Before injection of contrast |  |  | 
Before Contrast | w | w | w-w
 | 1576.5 | -221.1 | 233.3
Before Contrast |  |  | 
 | 1576.5 | -221.1 | 233.3
After / Contrast | w | w | w-w
 | 875 | -1876 | 914
 | 875 | -1876 | 914
[1] Institute of Nuclear Physics Polish Academy of Science, Kraków, Poland
[2] University of Alberta, Department of Oncology, Edmonton, Canada
[3] University of Calgary, Health Science Center, Calgary, Canada
Images before Injection of T1/T2 Contrast Agent: